## Slide 1
Crystalline Insulators
(bandgap >4 eV by convention)
The transmission spectrum for sapphire (Al2O3) shows the features typical of insulators and semiconductors.
There is high transmission in the transparency range of the crystal and lies in the bandgap, here in the wavelength range 0.2-6.0 μm.
Hence, sapphire is colourless and transparent to the eye.
Optical properties of materials - introduction
Chapter 4

## Slide 2
The transparency drops sharply in the UV for λ < 0.2 μm due to absorption by bound electrons).
The dip in the transmission at ~3 μm, and the sharp drop in transmission for λ > 6 μm, is caused by vibrational absorption and is not related to the electronic band structure.
Chapter 4

## Slide 3
Main point:
Fundamental absorption edge arises from absorption from conduction band to valence band.
nearly
imaginary
nearly
real
Chapter 4

## Slide 4
Some crystalline insulators
at 546 nm
Chapter 4

## Slide 5
Some crystalline semiconductors
at 10 µm
Note the correlation between the short wavelength limit of the transparency range and the refractive index
Chapter 4

## Slide 6
Most glasses are made by fusing sand (silica: SiO2) with other chemicals (choice determines refractive index and dispersion). They exhibit optical properties of typical insulators but are not crystalline.
As an amorphous solid, the atomic structure of glass lacks any long range translational periodicity.
However, the local chemical bonding constrains the possible atomic positions so that glasses do possess a high degree of short-range order. In silica there is a tetrahedral arrangement of oxygen atoms around the silicon atoms
Glasses
Chapter 4

## Slide 7
Doped glasses and crystalline insulators
Coloured glass filters and stained glass are made by the addition of semiconductors and other dopants.
Notre-Dame de Paris rose window
Colour control by:
Varying the composition of the dopant. e.g. an alloy semiconductor, like CdxZn1-xSe where the bandgap is tuned by x.
(b) Changing the size of semiconductor crystallites (quantum dots) within the glass. Quantum size effects occur when crystallite size is comparable to electron wavelength and change the bandgap.
Chapter 4

## Slide 8
Ruby: Al2O3 with 0.05% Cr3+ - appears
red because absorbs in blue and yellow/green
Transition metal and rare earth ions are used extensively to dope glasses and insulating crystals for solid state lasers. Transition metals also give colour to gemstones. The discrete optical transitions of isolated atoms are broadened to give absorption bands.
Chapter 4
Ti-doped
sapphire

## Slide 9
Metals
Reflectivity of silver from the infrared to the ultraviolet. [Fox, fig. 1.5]
Metals have a high reflectivity in the visible, below a characteristic frequency called the plasma frequency, due to interaction of light with free electrons.
For silver, the reflectivity is close to 100% in the infrared.
The reflectivity starts to fall in the visible spectrum where interband transitions (responsible for metal colour) occur and drops sharply in the ultraviolet – where metals are transparent.
Chapter 4

## Slide 10: Molecular materials
Organic compounds (those based on C-C bonds) can be crystalline or
amorphous. Covalent bonds within molecules are strong but molecules
are bonded to each other by weak van der Waal’s forces so that optical
properties of molecular solids are similar to those of constituent molecules.
Electronic and vibrational states are strongly
localised on molecules and strongly coupled
to each other.
Organic light emitting diode
Organic materials can be classified as
saturated : valence electrons form strong localised bonds between atoms;
conjugated: bonding is based on delocalized orbitals spread over whole molecule; weaker.
Chapter 4

## Slide 11: Photoluminescence (PL)
Semiconductor picture: recombination of conduction band (CB) electron with valence band (VB) hole.
So, would expect energy of PL to be that of the (direct) band gap EG (as measured by absorption measurements).
In fact, in crystalline semiconductors, photon emission at EG is quite rare: often, free electrons and holes relax into (i) excitonic or (ii) defect or impurity-related states more quickly than any direct recombination process. These emit light at lower energies.
Chapter 4
Notes: Semiconductor picture vs molecular picture; intrinsic versus defect

## Slide 12
Excitons
Excitons are electron-hole pairs bound by Coulomb attraction – similar to
a hydrogen atom with swap of proton for hole: different reduced mass m and also e.
Band-edge optical properties can be dominated by excitons in 2 dimensional materials (because e is very small) and ones with large m (so having flat bands).
Chapter 4
Small µ
Large εr
Large µ
Small εr
3D semiconductors
Insulators(e.g. alkali halides)
Molecular crystals

## Slide 13
Exciton features in absorption
Chapter 4
GaAs
Eg =1.425 eV
RX = 4.2 meV
n=1

## Slide 14
T Kazimierczuk et al. Nature 514, 343-347 (2014) doi:10.1038/nature13832
High-resolution absorption spectra of excitons in Cu2O.
Chapter 4

## Slide 15
g
t
n
g = generation rate
t = lifetime
Energy
Chapter 4
PL basics (1)

## Slide 16: PL basics (2)
g
tR
n
tNR
R = radiative
NR = non-radiative
Radiative and non-radiative lifetimes are often strongly dependent on temperature. Temperature also affects re-excitation from B back to A.
A
B
Chapter 4

## Slide 17
PJ Dean et al, PRB 4 (1971) 1926
Excitons can themselves bind to impurities (donors, acceptors) especially at low temperatures; analogous to H2.
These spectra show the PL of GaP doped with Zn (top) and Be (bottom)
(Dean et al., 1971)
Chapter 4
Exciton and impurity-bound exciton features in emission